## Slide 1
Stress and Strain Transformations
Textbook Chapters 9, 10
Jiangyu Li
SUSTech
Mechanics of Materials

## Slide 2
Uniaxial Tensile Test
What can we learn from here?

## Slide 3
Fracture Surface: Tension
Why is there a difference, and what causes it?

## Slide 4
Fracture Surface: Torsion
Why is there a difference, and what causes it?

## Slide 5
Multi-axial Load: Yielding
-
-
Why is there a difference, and what causes it?

## Slide 6
What is Stress?
Force per unit area?
What force? What area?

## Slide 7
Effect of Orientation

## Slide 8
Effect of Orientation

## Slide 9
3D Stress
First index: area
Second index: direction

## Slide 10
2D Stress

## Slide 11
Sign Convention
Positive: acting on positive (negative) plane, along positive (negative) direction

## Slide 12
Effect of Orientation

## Slide 13
Effect of Orientation

## Slide 14
Stress Transformation

## Slide 15
Free Body Diagram

## Slide 16
Free Body Diagram

## Slide 17
Equilibrium

## Slide 18
Stress Transformation
Constant trace

## Slide 19
Example

## Slide 20
Example

## Slide 21
Example

## Slide 22
Extreme Values

## Slide 23
Extreme Values

## Slide 24
Example

## Slide 25
Example

## Slide 26
Example

## Slide 27
Example

## Slide 28
Example

## Slide 29
Example

## Slide 30
Extreme Values: Torsion
=0: ductile
= ∞ : brittle

## Slide 31
Example

## Slide 32
Example

## Slide 33
Extreme Values: Uniaxial Tension
=0: brittle
=∞: ductile

## Slide 34
Example
Use different coordinate?

## Slide 35
Example
Maximum?

## Slide 36
Example
Maximum?

## Slide 37
Stress Transformation
Constant trace

## Slide 38
Mohr’s Circle

## Slide 39
Mohr’s Circle

## Slide 40
Mohr’s Circle

## Slide 41
Example

## Slide 42
Example

## Slide 43
3D Mohr’s Circle
Don’t forget the third dimension

## Slide 44
Example
Consider a point where the stress components are indicated in the given stress element in x-y coordinate.
After rotating to x’-y’ coordinate, it is found that normal stress along y’-plane is compressive and its magnitude is 100MPa.
Determine the normal stress acting on x’-plane.

## Slide 45
Example

## Slide 46
Example

## Slide 47
Example

## Slide 48
Strain

## Slide 49
Normal and Shear Strains

## Slide 50
Sign Convention

## Slide 51
3D Strain

## Slide 52
Plane Strain

## Slide 53
Strain Transformation

## Slide 54
Stress Transformation
Constant trace

## Slide 55
Strain Transformation

## Slide 56: Example

## Slide 57: Principal Strain

## Slide 58: Maximum Shear Strain

## Slide 59: Example

## Slide 60: Example

## Slide 61: Maximum Shear

## Slide 62: Maximum Shear

## Slide 63: Strain Rosette

## Slide 64: Strain Rosette

## Slide 65: Strain Rosette

## Slide 66: Assignment
Due May 12
Textbook
9.8, 9.13, 9.14, 9.20, 9.51, 9.84, 9.88
10.2, 10.5, 10.26