## Slide 1
Fracture Mechanics
Mechanical Behavior of Materials
Chapter 8.1-8.4, 8.7
Jiangyu Li
Mechanics of Materials

## Slide 2
Fracture

## Slide 3
Failure Criteria
Materials assumed to be perfect:
  Brittle Materials
    Max Normal Stress
  Ductile Materials
    Max Shear Stress
    Octahedral Shear Stress
Materials have flaw or crack in them:
  Linear Elastic Fracture Mechanics (LEFM)
    Stress intensity factor (K) describes the severity of the existing crack condition
    If K exceeds the Critical stress intensity (Kc), then failure will occur

## Slide 4: Stress Intensity Factor

## Slide 5: Effect of Crack Length
2014-T6 aluminum

## Slide 6: Stress Intensity Factor: Tension

## Slide 7: Geometry Factor F

## Slide 8: Example
AISI 1144 Steel
Central crack
b=40mm
t=15mm
If a=10mm,
Maximum P with safety factor 3?
How about a=24mm?
At what crack size will yielding occur first? 540MPa
66MPa.m0.5

## Slide 9
Example
2014-T651 Aluminum
Central crack
b=50mm
t=5mm
P=50kN
Kic=24MPa m 1/2
At what crack size will fracture occur?

## Slide 10: Stress Intensity Factor: Bending

## Slide 11: Geometry Factor F

## Slide 12: Example
Kc=3.0 Mpa m0.5
b=20mm; t=10mm;
Safety factor 2.5
M=10N.m
What is the largest crack length allowable?

## Slide 13: Superposition

## Slide 14: Effect of Crack Length
2014-T6 aluminum

## Slide 16: Brittle vs. Ductile Behavior
Steel AISI 1144: 840MPa
300-M: 2010
66 MPa.m0.5
2010 MPa

## Slide 17: Plastic Zone

## Slide 18: K field
Plane stress
Plane strain

## Slide 19: Limitation of LEFM
Plane strain
-
-

## Slide 20: Example
Central crack
a=10mm
b=50mm
t=5mm
Large h
P=50 kN
so=415 Mpa
Determine whether plane strain or LEFM apply, plastic zone.

## Slide 21: Effect of Temperature and Rate

## Slide 22: Effect of Temperature and Rate

## Slide 23: Brittle Failure

## Slide 24: Double Bonus Quiz
Which of the following statements are incorrect:
Larger stress leads to longer transition crack length at
High strength material is more vulnerable to crack
Transition crack length at does not depend on ultimate strength
Linear elastic fracture mechanics does not apply to cracks shorter than at

## Slide 25: Assignment
Mechanical behavior of materials:
8.4, 8.10, 8.15, 8.47