## Slide 1
Fatigue
Mechanical Behavior of Materials Sec. 9.1, 9.2, 9.6-9.8
Jiangyu Li
Mechanics of Materials

## Slide 2
0.2Hz, 6.3M cycles a year!

## Slide 3: Static Failure
Load is applied gradually
Stress is applied only once
Visible warning before failure

## Slide 4: Cyclic Load and Fatigue Failure
Stress varies or fluctuates, and is repeated many times
Structure members fail under the repeated stresses
Actual maximum stress is well below the ultimate strength of material, often even below yield strength
Fatigue failure gives no visible warning, unlike static failure. It is sudden and catastrophic!

## Slide 5: Characteristics
Primary design criterion in rotating parts.
Fatigue as a name for the phenomenon based on the notion of a material becoming “tired”, i.e. failing at less than its nominal strength.
Cyclical strain (stress) leads to fatigue failure.
Occurs in metals and polymers but rarely in ceramics.
Also an issue for “static” parts, e.g. bridges.
Cyclic loading stress limit<static stress capability.

## Slide 6: Fatigue Failure Feature
Flat fracture surface, normal to stress axis, no necking
Stage one: initiation of microcracks
Stage two: progress from microcracks to macrocracks, forming parallel plateau-like facture feature (beach marks) separated by longitudinal ridge
Stage three: final cycle, sudden, fast fracture.
Bolt, unidirectional bending

## Slide 7: Fracture Surface

## Slide 8: Characteristics
Most applications of structural materials involve cyclic loading; any net tensile stress leads to fatigue.
Fatigue failure surfaces have three characteristic features:
  A (near-)surface defect as the origin of the crack
  Striations corresponding to slow, intermittent crack growth
  Dull, fibrous brittle fracture surface (rapid growth).
Life of structural components generally limited by cyclic loading, not static strength.
Most environmental factors shorten life.

## Slide 9: Fatigue-Life Method
Stress-life method
Facture mechanics method

## Slide 10: Stress-Life Method
Specimen are subjected to repeated forces of specified magnitudes while the cycles are counted until fatigue failure

## Slide 11: Stress Cycle
A stress cycle (N=1) constitute a single application and removal of a load, and then load and unload in the opposite direction

## Slide 12: Alternating Stress
a = (max-min)/2
m = (max+min)/2

## Slide 13: S-N Diagram
The greater the number of cycles in the loading history, the smaller the stress that the material can withstand without failure.

## Slide 14: S-N Diagram
The higher the mean stress, the shorter the fatigue life.

## Slide 15: S-N Diagram

## Slide 16: S-N Diagram
Endurance limit

## Slide 17: Endurance Limit
Table A-24
For steel

## Slide 18: S-N Diagram
Aluminum

## Slide 19: Fatigue Life

## Slide 20: Safety Factor

## Slide 21: Example
9.10 For AISI 4340 steel in Table 9.1, a life of 1.94x105 cycles to failure is calculated for the stress amplitude of sa=500 Mpa. Suggestion is made that parts of this type be replaced when the number of cycles applied reach 1/3 of the life.
What is the safety factors in life and in stress
Is the suggestion good?
With safety factor in stress of 2, when should it be replaced
A=1643, b=-0.0977

## Slide 22: Effect of Mean Stress

## Slide 23: Effect of Mean Stress
Goodman
Gerber
Morrow

## Slide 24: Example
AISI 4340 steel is subjected to cyclic load with a tensile mean stress of 200 MPA
  What is the fatigue life for stress amplitude of 450 MPA
  How significant is the effect of mean stress?
  Estimate the relationship between stress amplitude and fatigue life for this mean stress
A=1643, b=-0.0977
sf’=1758
f'

## Slide 25: Safety Factor with Mean Stress

## Slide 26: Example
Man-Ten steel (sf’=1089MPa, b=-0.115) subject to stress amplitude of 180 Mpa and mean stress of 100PMa for 20000 cycles
  What is the safety factor in life and stress?
  When to replace if safety factor of 2 in stress?
f'

## Slide 27: Bonus Quiz
D
Identify where the fatigue crack initiates:
A
B
C
D

## Slide 28: Assignment
D
Mechanical behavior of materials:
9.10, 9.11, 9.21, 9.37

## Slide 29
Fracture Mechanics based Fatigue Analysis
Mechanical Behavior of Materials Sec. 9.1, 9.2, 9.6-9.8
Jiangyu Li
Mechanics of Materials

## Slide 30: Fatigue Failure Feature
Flat fracture surface, normal to stress axis, no necking
Stage one: initiation of microcracks
Stage two: progress from microcracks to macrocracks, forming parallel plateau-like facture feature (beach marks) separated by longitudinal ridge
Stage three: final cycle, sudden, fast fracture.
Bolt, unidirectional bending

## Slide 31: Paris Law
D

## Slide 32: Airplane Disaster
D
In January 1954, a de Havilland Comet, an early commercial jet airliner, broke up in flight and crashed into the Mediterranean Sea. In April of the same year, another Comet crashed in the waters near Naples, Italy.

## Slide 33: Airplane Disaster
D
Stresses in the metal skin had concentrated at the corners of square “windows,” and, following repeated cycling of cabin pressure, these stress concentrations opened cracks that suddenly grew the length of the fuselage, and the whole aircraft came apart.

## Slide 34: Paul Paris
D
Trained at Lehigh University in applied mechanics, Paris became a faculty associate at the Boeing Co. in the summer of 1955. Because Boeing was developing the first American commercial jet, Paris was asked to look into the Comet failures.
“I was scared to death,” he says. “I had never been in industry before, and they handed me this enormous task. I didn’t have the courage to tell them I didn’t know anything about fracture.”

## Slide 35: Paris Paper

## Slide 36: Paris Paper

## Slide 37: Paris Paper

## Slide 38: Paris Paper

## Slide 39: Paris Paper

## Slide 40: Fatigue Crack Growth
D

## Slide 41: Periodic Inspection
D

## Slide 42: Key Parameter
D

## Slide 43: Paris Law
D

## Slide 44: Effect of R
D

## Slide 45: Application
D

## Slide 46: Testing
D

## Slide 47: Testing
D

## Slide 48: Testing
D

## Slide 49: Effect of R: Walker Equation
D

## Slide 50: Effect of R: Walker Equation

## Slide 51: Life Estimate

## Slide 52: Paris Law

## Slide 53: Crack Length at Failure

## Slide 54: Example