## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower, Rm310
MSE 311: Thermodynamics of Materials
Lecture 8: Most Probable Distribution

## Slide 2
Thermodynamics free energy
Helmholtz Free Energy A, or F
----the energy that can be converted into work at a constant T and V
Thermodynamic free energy,
the energy in a physical system that can be converted to do work
Gibbs Free Energy G,
----the energy that can be converted into work at a constant T and P
throughout the system

## Slide 3
dU
dH
dG
dA
-d(TS)
+d(PV)
+d(PV)
Internal energy
Helmholtz Free Energy
Gibbs Free Energy
Enthalpy
-d(TS)
U,H, A, G

## Slide 4
Thermodynamics Venn diagram
American Journal of Physics 79, 950 (2011)
Grandcanonical Potential
Canonical Potential

## Slide 5
16. Boltzmann Equation
Chapter 4
Introduction of Thermodynamics, /6th Edition, CRC Press, 2018

## Slide 6
1853-1932
1844-1906
Energy VS Atom
Friedrich Wilhelm Ostwald
Ludwig Boltzmann
Noble Prize: 1909
Discover ring Nitric arcid
Ernst Mach
1838〜1916
Max Planck
1858-1933
Noble Prize: 1918
What the world made by：
The Ostwald-Boltzmann Controversy

## Slide 9
Classic Thermodynamics is phenomenological.
TD variables: T, V, P
It didn’t consider the properties of their constituent particles and the interactions between them.
Classic Thermodynamics
Statistic Thermodynamics
It consider the detailed information of the constituent particle by statistical methods, probability theory and the microscopic physical laws.
It provides a connection between the macroscopic properties of materials in thermodynamic equilibrium, and the microscopic behaviors and motions occurring inside the material.
Scope of Statistic Thermodynamics

## Slide 10
Disorder increases, entropy increases
Melting
Boiling
S = Hmelting/T
S = Hboiling/T
Latent heat of melting
H2O
Latent heat of evaporation
Entropy: the degree of disordering

## Slide 11
Degree of Mixed-up-ness
The mixing is a irreversible process
The mixed-up-ness describe the indeterminacy at a given location
How quantification of the term “degree of mixed-up-ness?

## Slide 12
Macrostates & Microstates
Straight flush
Microstates
Pick up any 5 card
Macrostate, i.e. flush
Macrostate, i.e. Straight flush

## Slide 13: Physics of wave
Wave is the propagation of a vibrational state, in which energy is transported without simultaneous mass transport.
Quantized energy level

## Slide 14: Standing wave in a string with two ends fixed
Since the fixed ends must always be nodes, the condition must be met is that the distance l between the fixed ends of the string must be an integral number of half wavelengths:
l = n or (n is a positive integer)

## Slide 15
In Quantum theory
If a particle is confined to move within a given fixed volume, then its energy is quantized, i.e., the particle may only have certain discrete allowed values of energy, which are separated by “forbidden energy bands.”
,
,
,
Quantized energy level of the particles or the crystal structure is
The ground state : ε0
The succeeding levels of increasing energy: ε1 , ε2 , ε3
Quantized energy level

## Slide 16
For the crystal contains n particles and has the energy U
statistical mechanics asks the questions:
In how many ways can the n particles be distributed over the available energy levels such that the total energy of the crystal is U, and, of the possible distributions, which is the most probable?
Quantized energy level

## Slide 17
Let’s say we have three identical particles, which are located on three distinguishable lattice sites A, B and C.
Let’s say the energy levels are equally spaced, with the ground level being taken as zero, the first level 1 = u, the second level 2 = 2u and the 3 = 3u. Let the total energy of the system be U = 3u
1
0
2
3
(a)
(b)
(c)
Most Probable Distribution
Three macrostates

## Slide 18
All three particles in level 1:
1 combinations
b. One particle in level 3, and the other two particles in level 0:
3 combinations
c. One particle in level 2, one particle in level 1, and one particle in level 0:
3 x 2 x 1 = 3! = 6 combinations
Consider three distinguishable lattice sites A, B and C.
Most Probable Distribution

## Slide 19
Microstate: knowing properties of all particles
Macrostate: knowing properties of the system
These distinguishable arrangements are called complexions or microstates,
and all of the 10 microstates correspond to a single macrostate.
Most Probable Distribution

## Slide 20
Let’s say we have a system of volume V, internal energy, U and temperature T, consists of n particles.
The particles can be atoms, molecules, which are structurally identical.
These particles are distributed in i energy levels (quantum theory)
Energy level
# of particles
e0
n0
e1
n1
e2
n2
……..
……..
ei
ni
ni = n, and eini = U
# of particles
n’0
n’1
n’2
……..
n’i
Distribution 1
Distribution 2
The number of combinations:
The number of total combination:
Most Probable Distribution
Combinatorics

## Slide 21
The earlier example:
Most Probable Distribution
The number of arrangement

## Slide 22
Find Most Probable Distribution
Find Most Probable Distribution
=Find set of ni, to maximize i = n!/(n1!n2!..ni!)
Stirling’s approximation: when X is very large: ln(X!)  XlnX -X
Any interchange of particles
If Ω has the maximum possible value then a small rearrangement of particles among the energy levels will not alter the value of Ω or of ln Ω
n is constant  δnlnn=0

## Slide 23
Find Most Probable Distribution
 is the constant with the units of reciprocal energy
Α is the dimensionless constant
Partition function

## Slide 24
Boltzmann’s distribution function
Boltzmann’s distribution function
Schematic representation of the most probable distribution of particles among the quantized energy levels.
kB is the Boltzmann constant

## Slide 25
Most Probable Distribution
One distribution have most probable arrangements, t
N << t, lnN << lnt: ln  lnt
So, we can use the most probable distribution to
describe the system, and neglect other distribution.

## Slide 26
Temperature Effect
Schematic representation of the most probable distribution of particles among the quantized energy levels.
Influence of temperature on the most probable distribution of particles among energy levels

## Slide 27
Internal energy increase with temperature
Higher temperature, higher energy levels become more populated, so the U increases
set of ni maximizes i = n!/(n1!n2!..ni!)
as the ni follow the Boltzmann temperature

## Slide 28
Boltzmann Equation
The system of n particles and heat bath with fixed U, V and n are in thermal equilibrium
Now let small amount of heat flow to the system, the  will change:
q = dU, constant volume:
dS = q/T
Boltzmann
equation
Entropy: S
Number of arrangement: Ω
1844-1906
Ludwig Boltzmann

## Slide 29
Configurational Entropy
4:0 = 1
2:2 = 36
1:3 = 16
(0:4 = 1)
(3:1 = 16)
Two crystal contact

## Slide 30
Configurational Entropy
A + B (unmixed)  A + B (mixed) at constant U, V and n
(state 1) (state 2)
Total mix
Before mix

## Slide 31
Configurational and thermal Entropy
Thermal entropy
or vibration entropy
Configurational
Entropy
Configurational entropy refers to the work done without an exchange in temperature,
Thermal entropy refers to the work done with the exchange in temperature.
Entropy is a measure of the randomness of a thermodynamic system. An increase in the randomness refers to the increase of the entropy and vice versa

## Slide 32
Configurational and thermal Entropy
Thermal entropy
or vibration entropy
Configurational
Entropy
Configurational entropy refers to the work done without an exchange in temperature,
Thermal entropy refers to the work done with the exchange in temperature.
Entropy is a measure of the randomness of a thermodynamic system. An increase in the randomness refers to the increase of the entropy and vice versa

## Slide 33
The vacancy concentration ?
Considering the formation energy of a vacancy: εV
The increase entropy equivalent to arrange N atoms and n vacancies on N+n lattice site:

## Slide 34: 17. Elastocoloric/ Electrocaloric/Magnetocaloric

## Slide 35
Wang et al., Science 366, 216–221 (2019)
A simple example

## Slide 36
Fig. 1. Twist-based mechanocaloric performance for single rubber fibers.

## Slide 37
Elasto-coloric effect in polymer
Rapid stretching or unstretching of a wide rubber band is nearly isentropic/ adiabatic process
The stretching decreases the configurational entropy Sconf (molecular structure becomes more ordered)
the stretching is isentropic, then the thermal/vibrational entropy Sth increase to compensate for the decrease of Sconf.
the heat generated by stretching is dissipated
T should decrease as a result of rapid unstretching

## Slide 38
European Polymer Journal , 2018, 99, 212–221
Elastocaloric - uniaxial stress
Barocaloric - hydrostatic P
Magnetocaloric - magnetic field
Electrocaloric - electric field
Elasto-caloric effect in polymer

## Slide 39: Elastocoloric Effect in metals
Large elastocaloric effect in a Heusler-type Co50V35Ga14Ni1 polycrystalline alloy
Appl. Phys. Lett. 118, 103904 (2021)

## Slide 40
Theoretically Considering Elastocaloric Effect
Helmholtz Free energy is chosen for the TD criteria
Applied Thermal Engineering 57 (2013) 33-38

## Slide 41
Helmholtz Free energy
Assuming that the heat transfer between the material and the ambient temperature
h: heat coefficient, Λ:surface, Text : room temperature
Applied Thermal Engineering 57 (2013) 33-38
Maxwell relation：
the evolution of the temperature exchangebetween natural rubber and the ambient environment as a functionof the mechanical elongation.

## Slide 42
Refrigerant capability (RC)
Applied Thermal Engineering 57 (2013) 33-38