## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower, Rm310
Lecture 14: Subregular solution
MSE 311: Thermodynamics of Materials

## Slide 2
34. The Statistic explanation II
Ref. Introduction of Thermodynamics of Materials, D. R. Gaskell, Chapter 9

## Slide 3
A-B-C ternary system solid solution has 6 types of Adjacent atomic pairs: A-A,B-B,C-C,A-B,B-C,C-A.
A-B-C ternary system solid solution
A-B binary system
z：the number of neighbor atoms

## Slide 4
For the XA=XB=XC=1/3
For n component system, Xi=1/n
High entropy alloy!!
A-B-C ternary system solid solution

## Slide 5
Tough and strong

## Slide 8
Consider atomic Ordering
Consider the ordering transformation of a random A – B solution phase
long-range order parameter (LRO), η [eta]
Xi=A,B, the fraction of the component I
Yj=α,β , the fraction of lattice site j
r j= α,β is the fraction of j sites that are “ rightly” occupied

## Slide 9
For the BCC (random) → B2 (ordering) transformation of equiatomic alloy,
Y α and Y β are 1/2 , X A= XB = 1/2.
Consider atomic ordering
Prove :
If all the α site are occupied by A atoms, rα = 1 and η=1
If all the α site are occupied by B atoms, rα = 0 and η=1
If all the α site are randomly occupied, rα = 1/2 and η=0

## Slide 11
Including Second-Neighbor Interactions
first-neighbor interactions energy
Second-neighbor interaction energies
the heat of transformation

## Slide 12
35. Subregular Solutions
Ref. Introduction of Thermodynamics of Materials, D. R. Gaskell, Chapter 9

## Slide 13
Excess Molar Gibbs Free Energy
- Excess value: different between its actual value and the value that it would have if the solution were ideal
G: molar Gibbs free energy of the solution
Gid: molar Gibbs free energy of the solution if it is ideal
GXS: excess molar Gibbs free energy
Gibbs free energy before mixing G’:
Gibbs free energy after mixing G’’:

## Slide 14
Excess Molar Gibbs Free Energy
For any solution
For Regular solution
For the solution with atomic ordering:

## Slide 15
Excess Molar Gibbs Free Energy
Regular Solution
if
then
If only configurational entropy is considered, then Δ S M < Δ S M ,id .
If, however, other aspects of entropy exist in the alloy (e.g., magnetic spins, defects, volume effects), Δ S M may be greater than Δ S M ,id .

## Slide 16
Subregular Solutions
If we make more flexible(suitable for more solutions)
For subregular solution, all factors except a and b are equal zero.
So
These figures are not symmetric at XA=0.5 any more

## Slide 17
If we know a and b,
we can determine the relationship between GXS and compositions by
To determine maxima and minima,
Subregular Solutions
Regular solution

## Slide 18
Subregular Solutions
Binary system

## Slide 19
Subregular Solution-Engineering approach
Ternary system
Hillert, 1980

## Slide 20
Subregular Solutions

## Slide 21
Effect of Temperature
regular
Subregular
The influence of temperature on the behavior of subregular solutions is accommodated by introducing a third constant, τ ,

## Slide 22
Numerical example
At 700 K, the activity of Ga in a liquid Ga– Cd solution of composition X Ga = 0.5 has
the value 0.79. On the assumption that liquid solutions of Ga and Cd exhibit regular
solution behavior, estimate the energy of the Ga– Cd bond in the solution. The molar
enthalpies of evaporation of liquid Ga and liquid Cd at their melting temperatures
are, respectively, 270,000 and 100,000 J.

## Slide 24
36. Sublattice solid solution
Ref. 第四章，材料热力学 郝世明，第二版，北京化工出版社
第三章，微观组织热力学，西泽泰二，化学出版社

## Slide 25
III-V Solid Solution
III Group: Al, In, Ga
V Group: P, As, Sb
Structure of GaAs

## Slide 26
III-V Solid Solution
3B-sublattice
5B-sublattice
Neighbor’s number
z’ = 4
z = 12
z = 12

## Slide 27
First neighbor
III-V Solid Solution
z’ = 4
Second neighbor
z = 12
z = 12
EAA
EBB
EAB
ECC
EDD
ECD
For the 1-3 pair, it has to be a neighbor of 1‘ that could C or D

## Slide 28
Consider other atoms
The total entropy

## Slide 29
Entropy
化合物组元熵
I-亚点阵列上的混合熵
II-亚点阵列上的混合熵
Gibbs free energy
General express for (A,B)m (C,D)n
组元自由能项

## Slide 30
Interstitial solid solution
Simple solid solution: only one set lattice
Interstitial solid solution: two set sub-lattice
Entity sub-lattice , Fe, Cr, Mn, Mo
Void sub-lattice , C, O, H

## Slide 31
Interstitial solid solution
Relationship of the Solid solution composition and sub-lattice composition ?
γ-solution of Fe (fcc)
(Fe, Cr, Ni)1 (C, Va)1
Entity sub-lattice
Void sub-lattice
Va: vacancy
Solid solution:
FeCrNiC
Sublattice model:
Fraction of element: XFe + XCr +XNi+XC =1
yFe + yCr +yNi=1
yC+ yVa =1

## Slide 32
Interstitial solid solution
Relationship of the Solid solution composition and sub-lattice composition ?
α-solution of Fe (bcc)
(Fe, Si, Mo)1 (C, Va)3
Entity sub-lattice
Void sub-lattice
Va: vacancy
Solid solution:
FeSiMoiC
Sublattice model:
Fraction of element: XFe + XCr +XNi+XC =1
yFe + ySi +yMo=1
yC+ yVa =1

## Slide 33
γ-solution of FeCrNiC (fcc)
(Fe, Cr, Ni)1 (C, Va)1
α-solution of FeSiMoC (bcc)
(Fe, Si, Mo)1 (C, Va)3
Mixing entropy
Ma Nb
Hypothetical
compound
Question: calculate the mixing entropy of α-solution of FeSiMoC ?
Based the regular solution
For 1 mol M sub-lattice:
For 1 mol N sub-lattice:
For 1 mol MaNb:
For 1 mol α-solution :

## Slide 34
Mixing Enthalpy
α-solution of FeSiMoC (bcc)
(Fe, Si, Mo)1 (C, Va)3
Ma Nb
For 1 mol M sub-lattice:
For 1 mol N sub-lattice:
For 1 mol MaNb:
For 1 mol α-solution :