## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower, Rm310
Lecture 9: Specific heat
MSE 311: Thermodynamics of Materials

## Slide 2: 18. Statistical ensembles
Chapter 2， 徐祖耀，材料热力学，高等教育出版社，2008
Chapter 4， Gang Chen, Nanoscale Energy Transport and Conversion, Oxford, 2005

## Slide 3
1902, J. Willard Gibbs proposal the concept of statistical ensemble
Josiah Willard Gibbs
1839-1903
Statistical ensembles
Statistical ensemble: an idealization consisting of a large number of virtual copies (sometimes infinitely many) of a system, considered all at once, each of which represents a possible state that the real system might be in.
A statistical ensemble is a probability distribution for the state of the system
Gibbs, Josiah Willard (1902).
Elementary Principles in Statistical Mechanics. New York

## Slide 4
In an actual experiment, we usually need consider a time-averaged behavior for a system by solving Newton’s equation of motion or time dependent Schodinger Equation
The introduce of statistical ensemble avoid the time average
Ergodic hypothesis （遍历假设）
The ensembles average of a observed quantity is equal to the time average of the same quantity.

## Slide 5
Canonical
Ensemble
Microcanonical
Ensemble
isolated systems
close systems
Grandcanonical
Ensemble
open systems
TD potential
Partition function
Probable
Distribution
Ensemble

## Slide 6
Thermodynamics Potential
Canonical
Ensemble
Microcanonical
Ensemble
isolated systems
close systems
Grandcanonical
Ensemble
open systems
TD potential
U and H are also thermodynamics Potential.
This is not Gibbs free energy

## Slide 7
Thermodynamics Venn diagram
American Journal of Physics 79, 950 (2011)
Grandcanonical Potential
Canonical Potential

## Slide 8
The Bose-Einstein Distribution
For other case, such as gas molecules, can have a fixed number of particles
We should use grand canonical ensembles as Fermions
The general Bose-Einstein distribution
The general Fermi-Dirac distribution
The general Maxwell-Boltzmann distribution
Notes: Darwin–Fowler method

## Slide 9: 19. Statistical thermodynamic interpret of Heat capacity
Chapter 4 and 5, Introduction to Solid State Physics, C. Kittle, Wiley, 2004

## Slide 10: Heat capacity: cV and cP
Constant Volume Process (CV):
Constant Pressure Process (CP):
dU = dq – dW = dq
dH =dU+pdV= dq
or dU=CvdT
or dH=CPdT

## Slide 11: Heat Capacity: cV and cP
Represents the work done by the system per degree rise in temperature in expanding against the constant external pressure P acting on the system
Represents the work done by the system per degree rise in temperature in expanding against the internal cohesive forces acting between the constituent particles of the substance
For idea gas

## Slide 12: Dulong-Petit Rule
3R rule for the thermal conductivity!
Experimental shows that
3R rule is only valid as T is high enough
Cv is temperature dependent

## Slide 13
Equipartition of energy
each degree of freedom would have an average energy in the amount of kBT/2
The possible degree of freedom include: translation, rotation and vibration
Internal energy and specific heat
The monatomic gas
The diatomic gas
N2O: f=13
H2O: f=12
More complicate molecular
Open question

## Slide 14
Specific heat of H2
Transitional
part
Rotational
part
Vibration
part
rotational temperature of a hydrogen molecular is 85.3 K,
vibrational temperature is 6332K

## Slide 15: Einstein model
A crystal containing n atoms, each atom behaves as a harmonic oscillator vibrating independently about its lattice point.
As the behavior of each oscillator is not influenced by the behavior of its neighbors, each oscillator vibrates with a single fixed frequency v
A system of such oscillators is called an Einstein crystal.
Einstein model, 1907
Frequency
Wave Vector
Γ

## Slide 16
As each oscillator has three degrees of freedom, i.e., can vibrate in the x, y, and z directions,
the energy, U’, of the Einstein crystal (which can be considered to be a system of 3n linear harmonic oscillators) is given a
Einstein model
Quantized energy
Partition function

## Slide 17
Einstein model
Defining hv/k=θE, where θE is the Einstein characteristic temperature,
n equal to Avogadro’s number Na, nkB =R

## Slide 18
Einstein model of cV
Experimental data
as T/θ increases, Cv→ 3R , in agreement with Dulong and Petit’s law,
as T → 0, Cv→ 0, which is in agreement with experimental observation.
There is some discrepancy between experimental data and Einstein’s model
because of the assumption the oscillators vibrate with a single frequency

## Slide 19
Nature 395, 876 (1998)

## Slide 20
Debye model of cv
Peter Debye
1884-1966
Nobel Prize in Chemistry 1936
Frequency
Wave Vector
Γ
linear dispersion relationship
Cut-off frequency: ωD
Cut-off frequency: kD
Angular
frequency
Wave
vector
Phonon
velocity
Einstein’s assumption:
the assumption the oscillators vibrate with a single frequency
Debye’s modification:
the oscillators vibrate with in a rang of frequency
Wave
vector

## Slide 21
Debye model of cv
frequency distribution function of vibration mode
D(ω)
linear dispersion relationship
number of phonons
distribution
density
volume of spherical shell
number of phonons
Frequency distribution
Debye Frequency

## Slide 22
Thermal equilibrium occupancy of wavevector k
It follows the Bose-Einstein distribution
<n(ω)>
Debye model of cv
Debye Frequency
Debye heat capacity function contains
only one parameter Debye temperature.
The factor of 3 accounts for
the three phonon polarizations.

## Slide 23
Debye model of cv
Figure 6.3 The constant-volume molar heat capacities of several solid elements. The curves are the Debye equation with the indicated values of θD.
The materials with heavier atom has smaller θD

## Slide 24
Debye model of cV
Debye’s T3 –Law
for low temperature heat capacity
Some limitation of Debye’s mode:
The introduction of cut-off seems very arbitrary，not make sense
Linear dispersion relationship is not true at high wave vector

## Slide 25
20. Sine dispersion relation

## Slide 26
Einstein’s assumption:
the assumption the oscillators vibrate with a single frequency
Debye’s modification:
the oscillators vibrate with in a rang of frequency
A real dispersion relationship

## Slide 27
Acoustic phonon Vs. Optical Phonon

## Slide 28
Phonon Spectrum of Si

## Slide 29
Solution of Phonon dispersion relationship
Disperse as longitudinal wave
Disperse as transverse wave
Total force on s plane from s+1 and s-1 plane
Hooke’s law
The equation of motion
Solution
The equation of motion
The dispersion relation
G. Kittle, Introduction to Solid State Physics, Wiley, 2005

## Slide 30
Density of states
with sine dispersion relation
Assuming that the phonons of three –dimensional crystal obey the following isotopic dispersion relationship
The density of states
From the sine dispersion relation
The number of states
Group velocity
Phase velocity
From the line dispersion relation

## Slide 31
Heat capacity
with sine dispersion relation
Standing wave condition

## Slide 32
Linear dispersion
Sine dispersion
as k<< kc
Heat capacity
with sine dispersion relation
Notes: arcsin x = sin-1 x ， sin( arcsin x ) = x

## Slide 33
Pei’s mode covering both the features
of Einstien’s model and Debye’s mode
Heat capacity
with sine dispersion relation

## Slide 34
David G. Cahill
The relax time is equal to the half of the vibration circle
Lattice thermal conductivity reach the minimum
Estimation of lattice thermal conductivity

## Slide 35
Over estimated ~40%
Debye-Slack
Debye-Snyder
Estimation of lattice thermal conductivity

## Slide 36
n=1
n=2
n=3
n=4
n=5
n=6
Sine + Constant dispersion assumption

## Slide 37
Estimation of lattice thermal conductivity

## Slide 38
Pei used the linear dispersion approximation
And give a lower κmin
Estimation of κmin
Frequency
Wave Vector
Γ
Linear dispersion
Frequency
Wave Vector
Γ
Sine dispersion

## Slide 39
21. Other contribution to heat capacity

## Slide 40
The heat capacity of matter at low temperature
1. Lattice heat capacity
2. Electronic heat capacity
3. Magnetic heat capacity
4. Heat capacity anomalies
1800 Black first proposed the concept of heat capacity
1819 Dulong-Petit Law
1907 Einstein Model
1912 Debye Model
1928 Electronic heat capacity - Sommerfeld
1963 Rosenberg proposed the Schottky anomaly of heat capacity in solids
1980 Magnetic heat capacity - Sinha and Kumar
1992 Elliott discovered the Boson peak anomaly in heat capacity
2010-2020 Calorimetry, New model and Application
Notes: 从研究历史也可以发现固体的比热大致包含以下几类：晶体比热、电子比热、磁比热、异常比热
1800布莱克首次提出比热的概念
1819杜隆泊替定律
1831纽曼-科普定律进一步发展了杜隆泊替定律
1907年随着低温技术的发展，随着温度的降低，比热迅速减小，爱因斯坦基于量子理论提出了爱因斯坦模型
1912年，随着温度的进一步降低，在20K以下，爱因斯坦模型和实验结果差别较大，德拜提出德拜模型
1928年索末菲提出自由电子气模型，并由此推导出了电子比热
1963年，Rosenberg提出了固体中的肖特基异常比热
1980年，Sinha and Kumar在前人的基础上系统的提出了各种磁作用的比热
1992年，Elliott首次发现了波色峰
2010-2020进入21世纪，比热的研究主要集中在量热学、新型比热拟合模型的开发、比热在物理现象解析中的应用

## Slide 41
Variation of the Fermi-Dirac distribution function with at three temperatures.
Electronic heat capacity
Single particle density of states for free electrons. At T<< only those electrons within the range of the Fermi energy contribute to the specific heat.
When a gas consisting of N electrons (N is assumed to be very large) is in thermal equilibrium the probability that a particular energy level e is occupied is given by the Fermi-Dirac distribution function
is the density of states at the Fermi level. The numerical value of the above integral is and hence:
Kittel C., McEuen P., McEuen P. Introduction to Solid State Physics[M]. Wiley, New York, 1976, Vol. 8

## Slide 42
Magnetic heat capacity
The heat capacity of Fe4(P2O7)3 around magnetic transition
Paramagnetism, (b) Ferromagnetism,
(c) Antiferromagnetism, (d) Ferrimagnetism
There is a dispersion relation between the frequencies of different phases and the number of spintrons at these frequencies.
Ferromagnetism
Antiferromagnetism
Ferromagnetism
Antiferromagnetism
Fisher R. A., Bouquet F., Phillips N. E., et al. Physical Review B, 2001, 64: 134425.

## Slide 43
Heat capacity anomaly: Schottky anomaly
Schottky anomaly with different values
Klotz S., Steinle-Neumann G., Strässle T., et al. Physical Review B, 2008, 77: 012411.

## Slide 44
Boson peak anomaly
Low-temperature boson heat capacity peaks:
as-cast set and crystalline set,
partial enlargement of the as-cast set,
annealed set
partial enlargement of the annealed set.
Gil L., Ramos M., Bringer A., et al. Physical Review Letters, 1993, 70: 182.

## Slide 45
陈难先院士
At the low T limit
At the high T limit

## Slide 46: 22. Engineering considering of heat capacity

## Slide 47
The Empirical representation of heat capacity
The experimentally measured variation of the constant-pressure molar heat capacity of a material with temperature is normally fitted to an expression of the form

## Slide 48
The Empirical representation of heat capacity
1478-2670K
298-2670K
heat capacities (cp ) increased with temperature
heat capacities (cp ) of some elements which exhibit allotropy and some compounds which exhibit polymorphism.

## Slide 49
Partial liquid-like sub-lattice

## Slide 50
Temperature dependent Cp
Regular materials
Cu2Se
500K
700K
900K
1100K
Acta Materialia，2015

## Slide 51
Entropy as a function of temperature
For a closed system of fixed composition
undergoing a change in temperature from T1 to T2 at the constant pressure P
cp
T1
ΔH
T2

## Slide 52
Enthalpy-Temperature diagram
Considering a melting process
If Δcp=0, then ΔHT1 = ΔHT2
Kirchhoff ’s Law

## Slide 53
Enthalpy as a function of temperature
When a system undergoes a chemical reaction or a phase transformation at constant temperature and pressure, e.g.,
A+B=AB
ΔH is the difference between the enthalpy of the products of the reaction (the state 2), and the enthalpy of the reactants (the state 1), i.e
Endothermic process: ΔH is positive
Exothermic process: ΔH is negative

## Slide 54
H does not have an absolute value (only changes in H can be measured)
This convention assigns the value of zero to the enthalpy of elements in their stable states at 298 K (25°C)
The T-dependent heat of chemical reaction
Enthalpy-Temperature diagram

## Slide 55
(a). 298 to 600 K
(b). 600 K
(c). 600 to 1200 K
Prof. W.S. Liu | 55
Enthalpy-Temperature diagram

## Slide 56
Effect of pressure on the H and S
Apply dH=TdS+VdP, and thus
Maxwell’s equation
Maxwell’s equation
For a closed system of fixed composition undergoing changes in both P and T
Case-I
Case-II

## Slide 57
The third Law of Thermodynamics
For a closed system undergoing a reversible process, the Second Law gives
If the process is conducted at constant pressure, then
In 1906 Nernst postulated that, for chemical reactions between pure solids or pure liquids,
Nernst’s heat theorem states that
“for all reactions involving substances in the condensed state, ΔS is zero at the absolute zero of temperature.”

## Slide 58
The amendment of Nernst’s Statement
The incompleteness of Nernst’s theorem was pointed out by Planck, who stated that “the entropy of any homogeneous substance, which is in complete internal equilibrium, may be taken to be zero at 0 K.”
1. Glass
At temperatures lower than its equilibrium freezing tem-perature the glassy state is metastable with respect to the crystalline state,.
and a glass, not being in internal equilibrium, has an entropy at 0 K which is greater than zero by an amount which is dependent on the degree of atomic disorder in the glass
2 Solution
atomic mobility decreases exponentially with decreasing temperature, the maintenance of internal equilibrium becomes increasingly difficult.
Consequently a nonequilibrium degree of order can be frozen into the solid solution, in which case the entropy will not decrease to zero at 0 K

## Slide 59
Open questions:
1. Find a thermodynamic equation and discussion the possible limitation with in the dimension of space and time
2. Find some NEW example to discuss the reason why the 3nd Law of thermodynamics of Nernst’s theorem is failing, whether the Planks' modification solve your problem.
3. Discuss the possible case that needs modify the assumption of the Debye model for the heat capacity.
4. Find a new example to use the local vibrational mode to obtain the material with intrinsically low thermal conductivity.