## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower#, Rm310
Lecture 6 Heat Engine II
MSE 311: Thermodynamics of Materials
2022 Fall

## Slide 2: 11. Refrigeration Cycles
Ref. Thermodynamics: A Engineering approach, Chapter 10

## Slide 3
Refrigeration and our life
My life is given by the air-conditioning !!!

## Slide 4
Refrigerator
and air conditioning
History
1834: Jacob Perkins obtained the first patent for a vapor-compression refrigeration system.
1850: Alexander Twining, design and build vapor-compression ice machine.
1890s: refrigeration system began to appear in households
1930s: the vapor-compression refrigeration system become efficient, reliable, small, and inexpensive.
The first refrigerator Made-in China:
1955：天津医疗器械厂试制
1956: “雪花”冰箱
The first air-conditioning Made-in China:
1974：泰州市无线电元件九厂（春兰）， “雪松”窗式空调
1988: 华宝空调器厂, “雪莲”分离式空调

## Slide 5
Refrigerator
and air conditioning in China

## Slide 6
Bangladeshi air cooler
Adiabatic expansion  internal energy reduced reduced temperature
throttling

## Slide 7
Nozzles and Throttling valve
Energy balance of the steady-flow system
Enthalpy
Internal
energy
Flow
energy

## Slide 8
Joule-Thomson effect
The temperature change of a real gas or liquid (as differentiated from an ideal gas) when it is forced through a valve or porous plug while keeping it insulated so that no heat is exchanged with the environment.
μJ >0 temperature decrease after throttling
μJ =0 temperature no-change after throttling
μJ <0 temperature increase after throttling

## Slide 9
At 25 oC, if a gas following: PV=RT+6.4x104 P,
Considering a throttling at a pressure of 30MPa, asking the temperature will decrease or increase?
Jouel-Thomson effect

## Slide 10
Ideal Vapor-Compression Refrigeration Cycle
3
4
1
2

## Slide 11
Ideal Vapor-Compression Refrigeration Cycle
Enthalpy, H= U+PV

## Slide 13
Actual Vapor-Compression Refrigeration Cycle
Idea case
Actual case
Irreversibility:
Fluid frication
Heat transfer to surrounding
5
6

## Slide 14
Gas refrigeration cycle
Reversed Brayton cycles：
Brayton cycles

## Slide 15
Gas refrigeration cycle with regeneration

## Slide 17: 12. Silent power generator and refrigerator

## Slide 18
Silent power generator and refrigerator
How to get power in deep space when no enough light available?
How cooling the tiny the laser communicate device quietly?

## Slide 19
Satellite：Solar cell
Spaceship: RTG
Radioisotope thermoelectric generator

## Slide 20
Radioisotope Thermoelectric Generator
RTG made by Ukraine
嫦娥计划

## Slide 21
Thermoelectric Cooler for CPU
Thermoelectric Cooler for Telecom
Thermoelectric Cooler (TEC)

## Slide 22
Thomas J. Seebeck
German physicist
(1770-1831)
An electrical voltage was produced
by heating the junction between two different electrical conductors (e.g. Cu and Fe)
Seebeck Effect, 1821
A
B
S, Seebeck coefficient
eg.
Cu: +1.8 μV/K
Bi2Te3:+200 μV/K
Seebeck Effect

## Slide 23
Seebeck Effect
T.J. Seebeck,
Magnetische Polarisation der Metalle und Erze durch Temperatur-Differenz,
Abh. Deut. Akad. Wissensch. Berlin, Phys., Kl. (J. 1822-1823), p.265-373, 1825
Current Flow
Magnetic needle move
Bi
Cu
DV = a DT

## Slide 24
Peltier effect
Jean C.A.Peltier
French physicist
and watchmaker
(1775-1845)
Cooling was produced
at the junction of two dissimilar metals as a current pass it
Cooling
I
N-type
P-type
Π, Peltier coefficient
Peltier effect, 1834

## Slide 25
J.C.A. Peltier, Nouvelles Expériemences sur la Caloricite des courants électriques, Annales de Chimie et de Physique, 56, p.371-386, 1834
Peltier effect

## Slide 26
Thomson effect, 1855
William Thomson
1st Baron Kelvin
British physicist
(1824-1907)
Current, I
Tcold
Thot
Heat release/absorption, q
β, Thomson coefficient
Evaluation of heat when electric current passes through a single material that has a temperature difference along its length
Kelvin Relation
* He is widely known for determining the correct value of absolute zero as approximately -273.15 Celsius.
英国皇家“开尔文公爵”
Thomson effect

## Slide 27
TD of thermoelectric
generator and refrigerator
TH
TL
Efficiency of TEG
COP of TEC
I

## Slide 28
Efficiency of TEG
Efficiency of TEG
For simple, Assume:
T-independent S, σ, κ
Sn =-Sp, ρ n = ρ p, κ n = κ p
leg length =L, section= A
Wout
p
n
Qh
Qc
Th
Tc
I

## Slide 29
Efficiency of TEG
Wnet
p
n
Qh
Qc
Th
Tc
I
Efficiency of TEG

## Slide 30
Efficiency of TEG
Efficiency of TEG-updated
Set m=RL/R
Home work： finishing the derivation of ηmax for a thermoelectric generator, and thinking about whether the Joule heat term in the Qc could be less than ½ I2R,
if possible how to achieve it, if not why?
Figure of merit

## Slide 31
Efficiency of TEC
W
p
n
Qc
Qh
I
Refrigerator
Space, Tc
Warm
Environment, Th
COP of TEC

## Slide 32: 12*. TEG of a real device Considering T –dependent properties

## Slide 33
T –dependent thermoelectric properties

## Slide 34
Continuity equation of charge:
Current density:
Heat flux:
What if S, σ, κ are temperature dependent (common case for most materials)?
To answer this question, go back to the governing equation of the thermal-electric transport phenomenon
Energy conservation equation:
One dimensional governing equation
Efficiency of TEG– T dependent properties
H.K. Kim, W. S. Liu, Z.F. Ren, PNAS (2015), EES (2016)

## Slide 35
For T independent S, σ, κ
Integrating twice
x=0, T=Th
x=L, T=Tc
Exactly the previously given formula
Efficiency of TEG– T independent properties

## Slide 36
For T dependent properties
Integrating once
Integrating twice
x=0, T=Th
x=L, T=Tc
where
Efficiency of TEG– T dependent properties

## Slide 37
is found to be a good index for thermoelectric performance on the device level
Efficiency of TEG– T dependent properties

## Slide 38: 12**. TEG of a real system Considering external thermal resistance

## Slide 39
What if the boundary temperatures are unknown (common for real applications)?
External thermal resistances (of various levels) exist at the hot and cold sides of the TEG, which contract the effective from the total provided by the specific thermal environment
To answer this question, go back to the governing equation with general thermal boundary conditions
Efficiency of TEG– external thermal resistance
K Zhu, W. S. Liu, et al., EES (2020)
The Seebeck coefficient is denoted here as to avoid any confusion with the entropy term (S) which will appear later

## Slide 40
Exact solution for the effective temperature difference:
Both and are supposed to be solved here
But the cubic equation of is too complicated
So we need to simplify the temperature profile
Efficiency of TEG– external thermal resistance
The closed condition
Here is easily solved from a linear equation, thus the derivation could proceed
1st simplification

## Slide 41
Approximate solution for the system performance:
Efficiency of TEG– external thermal resistance
In the previous step, the temperature profile is over-simplified, leading to an error up to 15% for the output power
Here we need to get back some items in the term
Now accurate output power estimation (with errors within 4%)
1st simplification
2nd simplification

## Slide 42
The maximum efficiency and power of a TEG on the system level:
On the material level:
On the device level:
All in the similar form
Efficiency of TEG– on three levels

## Slide 43
Open Question
The assumption of ½ I2R is reasonable in real case?