## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower, Rm310
Lecture 13: Regular solution
MSE 311: Thermodynamics of Materials

## Slide 2
31. The behavior of non idea solutions
Ref. Introduction of Thermodynamics of Materials, D. R. Gaskell, Chapter 9

## Slide 3
Non-idea solution
A non-ideal solution is one in which the activities of the components are not equal to their mole fractions
A Raoultian ideal solution
For simple,
γi is activity coefficient
for idea solution
for nonidea solution
Both ai and γi depend on concentration
is always less than one
is less than one for nagative deviation solution
is larger than one for positive deviation solution
Raoult’s law
Henry’s law

## Slide 4
Figure 9.8 Activities in the system iron-nickel at 1600°C.
Figure 9.9 Activities in the system iron-copper at 1550°C
Negative deviation, γ<1
Positive deviation, γ>1
Gibbs-Duhem equation
Determining TD activity coefficient

## Slide 5
Nonidea solution
ideal solution
positive deviation from Raoultian behavior
negative deviation from Raoultian behavior
- Gibbs free energy
- The heat of mixing, if γi is temperature dependent
Gibbs-Helmholtz eq.

## Slide 6
In general, increasing the temperature of a nonideal solution causes a decrease in the extent to which its components deviate from ideal behavior
Nonidea solution
For positive deviation
The mixing is exothermic
The A-B bonding is more negative than that of A-A and B-B
For negetive deviation
The mixing is endothermic
The A-B bonding is less negative than that of A-A and B-B
eg. Fe-Ni
eg. Fe-Cu

## Slide 7
Henry’s law
(b): A-B bonding is stronger than A-A
A-B is less-negative than A-A
Negative deviation
from Raoultian behavior
(a): A-B bonding is weaker than A-A
A-B is less-negative than A-A
Positive deviation
from Raoultian behavior
For positive deviation
The mixing is endothermic
For negetive deviation
The mixing is exothermic

## Slide 8
The enthalpy, being determined by the relative magnitudes of the bond energies, attempts to either completely order (negative deviation from ideality) or completely un-mix (positive deviation from ideality) the solution
The entropy factor attempts to maximize the randomness of mixing of the atoms in the solution
Enthalpy VS. Entropy

## Slide 9
Determining TD activity
---application of Gibbs -Duhem
Two infinity tails
As XB  1, aB  1, and XB/XA  infinity
As XB  0, aB  0 and XB/XA  minus infinity

## Slide 10
Determining TD activity coefficient
-The minus infinity can be dliminated by considering activity coefficient

## Slide 11
Relationship between Herry's and Raoult's laws
Consider solute B in A-B solution follows Herry's law:
The range of composition over which the solute B obeys Henry's law, the solvent A obeys Raoult's law

## Slide 12
Direct Calculation of Integral Molar Gibbs Free Energy
Integrating between XA=0 and XA=XB
Can be applied to any state properties
Rearranging and dividing by XB2

## Slide 13
Calculation of ∆G from measured activity
Line b is the case for Raoults’s behavior
Line a
Line c
(a)
(c)

## Slide 14
Determining TD activity coefficient

## Slide 16
Measuring activity of Si in Si-Cu

## Slide 17
activity coefficient of Si in Cu-Si-Fe

## Slide 18
32. The regular solutions
Ref. Introduction of Thermodynamics of Materials, D. R. Gaskell, Chapter 8

## Slide 19
Regular solution
Thus far two classes of solution have been identified:
1. Ideal or Raoultian solutions in which
2. Nonideal solutions in which and
In 1895,Margules suggested that, at constant temperature, the activity coefficients of the components of a binary solution
Gibbs-Duhem equation:
We can demonstrate
For quadratic term alone
α i s T dependent
activity coefficients : γ
Activity: ai

## Slide 20
Regular solution
General nonideal solution
Regular solution
ΩAB: interaction parameter
is composition and temperature independent
Joel Henry Hildebrand
(1881-1983)
University of Pennsylvania
1949: Guggenheim, Rushbrooke, et al.
referenced the “regular solution” as

## Slide 21
Regular solution
Hilderbrand claims the original definition of regular solution
“A solution has a idea mixing entropy”
activity coefficients
Regular solution

## Slide 22
The change of enthalpy
of Regular solution
Nonidea solution
Regular solution
a; activity
γ: coefficient of activity
Ω: interaction parameter
Idea solution:
Non-dea solution:

## Slide 23
Regular solution
As XA  1, γA  1, A is a Raoultian solution
XB  0, γB  const., B is a Henrian solution
As XB  1, γB  1, B is a Raoultian solution
XA  0, γA  const., A is a Henrian solution
a; activity
γ: coefficient of activity
Ω: interaction parameter

## Slide 24
33. The Statistic explanation of regular solutions
Ref. Introduction of Thermodynamics of Materials, D. R. Gaskell, Chapter 8

## Slide 25
Statistics Model of Solutions
Consider 1 mole of a mixed crystal
containing NA atoms of A and NB atoms of B
Three types of atomic bond in the crystal:
A-A bonds, the energy of each of which is EAA
A-B bonds, the energy of each of which is EAB
B-B bonds, the energy of each of which is EBB
Bragg-William-Gorski (B-W-G model)
Nearest neighbor assumption: only the interaction between the nearest neighbors are considered
Random distribution: The atom A and B in the given lattice are totally random distribution:
Important assumptions:

## Slide 26
Statistics Model of Solutions
In the crystal, there are PAA A-A bonds, PBB B-B bonds are PAB A-B bonds,the total energy of the crystal
Let's say each atom has z nearest neighbors,
total number of bond to A
The factor 2 arises because of each A-A bound involve two A atoms

## Slide 27
Statistics Model of Solutions
Consider a pure crystal containing NA A, and each A has z nearest neighbors, The total bonds to A

## Slide 28
Statistics Model of Solutions
P: Pressure
Raoultian behavior
0
E
(EAA +EBB)/2
EAB
Positive
deviation
EAB
Negative
deviation

## Slide 29
Statistics Model of Solutions
If
In a solution which exhibits small deviations from ideal behavior
We can calculate PAB as follows
Consider two sites in the crystal:1 and 2.
The probability of 1 is occupied by A is XA.
Similarly, the probability of 2 occupied by B is XB
So the probability of form A-B pair is 2XAXB
the probability of form A-A pair is XA2
the probability of form B-B pair is XB2

## Slide 30
Statistics Model of Solutions
There are 1/2zNo pairs in 1mole of the crystal.
In a solution which exhibits small deviations from ideal behavior
Z: the number of nearest neighbors, or coordination number

## Slide 31
Statistics Model of Solutions
In a solution which exhibits small deviations from ideal behavior
activity coefficients
Regular solution

## Slide 32
Statistics Model of Solutions
Positive deviation
0
E
(EAA +EBB)/2
EAB
Positive
deviation
EAB
Negative
deviation
activity coefficients
Regular solution
Negative deviation

## Slide 33
Figure 9.25 Illustration of the origins of deviation from regular solution behavior.
As the entropy contribution to the Gibbs free energy is dependent on temperature, then
For any value of Ω, more nearly random mixing occurs as the temperature is increased
For any given temperature, more nearly random mixing occurs with smaller values of Ω.
Statistics Model of Solutions

## Slide 34
Mixing Entropy from Statistical model
The number of methods that randomly distribute NB B atoms to N lattice nodes is
B atoms can not be distinguished and A atoms only fill lattice nodes without B atoms, so
The number of microscopic configurations before mixing considers only the same kind of atoms, hence
Stirling’s approximation: when X is very large: ln(N!)  NlnN -N