## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower, Rm310
Lecture 16: Phase diagram-II
MSE 311: Thermodynamics of Materials

## Slide 2
42. Phase diagram – Partial solid solution
Chapter 10
Gibbs Free energy Composition and Phase diagrams of Binary System
Ref. Introduction to the thermodynamics of Materials, 6th edition, D. R. Gaskell, and D. E. Laughlin
Phase diagram of binary system
Complete liquid and solid solutions (idea solution)
Partial solid solution
Complete liquid miscibility and solid immiscibility

## Slide 3
Curve I: ideal solution
Effect of interaction parameter: Ω
Regular solution

## Slide 4
Complete solution
miscibility gap
Curve (mnopq):
The Gibbs energy to form a single solution
Line (mq):
The Gibbs energy to form a mixing of m and q
if the homogeneous solution of composition r separates into the two coexisting solutions m and q , the Gibbs free energy of mixing of the system is decreased from r to s .
Miscibility gap

## Slide 5
Criteria for the coexisted two phase
The equilibrium coexistence of two separate solutions at the temperature T and pressure P requires that
Ref
aA(in solution m)=aA(in solution q)
aB(in solution m)=aB(in solution q)
Criteria for the coexisted two phase
Equivalent Criteria for the coexisted two phase

## Slide 6
Criteria for phase stability

## Slide 7
Criteria for phase stability
XA= XB=0.5
α=2
α=2 is the critical value
α=2
α>2 phase separation
α<2 single phase
T>Tcr single phase
T<Tcr phase separation
Tcr is the critical temperature

## Slide 8
Criteria for phase stability in regular solutions
T>Tcr single phase
T<Tcr phase separation
The loci of the double tangent point
Miscibility gap
Equation of binodal curve
Equation of spinodal curve

## Slide 9
The effect of temperature on the activities of component αB derived from the ΔGM
Activities obtained from the intercepts, with the XB = 1 axis, of tangent drawn to the free energy curves as:
At T = Tcr and XB = 0.5,
the activity exhibits a horizontal inflexion
Criteria for phase stability in regular solutions
αB=XB

## Slide 10
Criteria for phase stability in regular solutions
Since at Tcr and XB = 0.5, both second and third derivatives of ∆GM with respect to XB are zero
Dash line bc: ∂aB/ ∂XB is negative
This is violates an intrinsic criterion for stability ∂ai/ ∂Xi >0
absolute
unstable

## Slide 11
Spinodal decomposition

## Slide 12
Spinodal decomposition
697
550

## Slide 13
43. Eutectic Phase diagram
Chapter 10
Gibbs Free energy Composition and Phase diagrams of Binary System
Ref. Introduction to the thermodynamics of Materials, 6th edition, D. R. Gaskell, and D. E. Laughlin
Phase diagram of binary system
Complete liquid and solid solutions (idea soludtion)
Partial solid solution
Complete liquid miscibility and solid immiscibility

## Slide 14
Phase diagrams
Partial solid solution
If any one of these conditions
is not met, then one or more two-phase regions will occur in the solid state
Complete mutual solid solubility
of A and B requires A and B
The same crystal structures
Comparable atomic size
Similar electronegativities and valences

## Slide 15
Phase diagrams, ΔG and a: T1
In Fig. 1b, a and d are for solid A and liquid B, which are standard states (G =0). b and c are for liquid A and solid B.
Fig. 1c is activity-composition relationships by using solid for A and liquid for B as standard states. Assuming the liquid solution follows Raoult’s law and the solid solution follows positive deviation from Raoult’s law.

## Slide 16
In Fig. 1b, a and c are for solid A and solid B, which are standard states (G =0). b and d are for liquid A and liquid B.
Fig. 1c is activity-composition relationships by using both solid A and B as standard states.
Phase diagrams, ΔG and a: T2

## Slide 17
In Fig. 1b, a and c are for solid A and solid B, which are standard states (G =0). b and d are for liquid A and liquid B.
Fig. 1c is activity-composition relationships by using both solid A and B as standard states.
Phase diagrams, ΔG and a: T3

## Slide 18
In Fig. 1b, a and c are for solid A and solid B, which are standard states (G =0). b and d are for liquid A and liquid B.
Fig. 1c is activity-composition relationships by using both solid A and B as standard states.
Phase diagrams, ΔG and a: T4

## Slide 19
Eutectic phase diagram

## Slide 20
Application

## Slide 21
Application
LL+ α  α
LL+ α  α α+β
Lα+β
Eutectic structure

## Slide 22
Nano precipitation for small thermal conductivity
Thermoelectric figure of merit
S: Seebeck coefficient
σ: electrical conductivity
κ: thermal conductivity

## Slide 23
44. Phase diagram-Complete liquid miscibility and solid immiscibility
Chapter 10
Gibbs Free energy Composition and Phase diagrams of Binary System
Ref. Introduction to the thermodynamics of Materials, 6th edition, D. R. Gaskell, and D. E. Laughlin
Phase diagram of binary system
Complete liquid and solid solutions (idea soludtion)
Partial solid solution
Complete liquid miscibility and solid immiscibility

## Slide 24
If the solubility is immeasurable small, A and B are insoluble.
In Fig. 1b, a and c are for solid A and liquid B, which are standard states (G =0). b and d are for liquid A and solid B.
Fig. 1c is activity-composition relationships by using solid A and B as standard states.
Phase diagrams, ΔG and a
any pure substance presents an infinite chemical sink to any other substance, or conversely, it is impossible to obtain an absolutely pure substance

## Slide 25
Activity-composition relationships by assuming the liquid solution follows Raoult’s law.
pqr is the activity of A with respect to pure solid A
s is the activity of pure solid A with respect to liquid A
str is the activity of A with respect to liquid A as the standard state
- Auvw is the activity of B with respect to liquid B as the standard state.
Phase diagrams, ΔG and a

## Slide 26
Calculate the liquid line
Of Complete liquid miscibility and solid immiscibility
Consider the equilibrium between Liquid and Solid
L+S
L: Raoultian liquid solution: aA(l) = XA(l)
S: pure solid A, XA(s)=1 and XB(s) =0

## Slide 27
45. Topological evolution of Phase diagram
Chapter 10
Gibbs Free energy Composition and Phase diagrams of Binary System
Ref. Introduction to the thermodynamics of Materials, 6th edition, D. R. Gaskell, and D. E. Laughlin

## Slide 28
Regular solution in both liquid and solid
Consider the binary system A–B which forms regular liquid solutions and regular solid solutions.The melting temperatures of A and B are, respectively, 800 and 1200 K.
As Tm,(A)<1000 K<Tm,(B), liquid is chosen as the standard state for A, and solid is chosen as the standard state for B. With reference to these standard states, the Gibbs free energies of mixing are:
for the liquid solutions and
The formation of idea liquid solution
The formation of idea solid solution

## Slide 29
Regular solution in both liquid and solid
for the solid solutions. Inserting the numerical data gives

## Slide 30
At temperatures lower than Tm,(A) and Tm,(B) solid is chosen as the standard state for both components:
Regular solution in both liquid and solid

## Slide 31
Regular solution in both liquid and solid
At temperatures lower than Tm,(A) and Tm,(B) solid is chosen as the standard state for both components:

## Slide 32
Regular solution in both liquid and solid
800K
700K
661K
601K
Phase diagram of binary system
Regular solution in both liquid and solid
500K

## Slide 33
Regular solution in both liquid and solid
Phase diagram of binary system
Regular solution in both liquid and solid
1203K
1150K
1090K
950K
789K

## Slide 34
Effect of Ωl and Ωs on the phase diagram

## Slide 35
Effect of Ωl and Ωs on the phase diagram
Topological changes
in the phase diagram
for a system A–B
with regular solid and liquid solutions
Ωl，[kJ]
Ωs，[kJ]
0
-10
-20
+10
+20
0
+15
+30
-15
L
L
L
L
L
L
L
L
L
L
L
L
L
α+α‘
α+α‘
L+L’
α+α‘
α+α‘
+30

## Slide 36
As is shown in the above Figure
the liquid solutions become increasing less stable relative to the solid phases with the consequence that the eutectic temperature is increased
0
-10
+10
+20
Ωs,l，[kJ]
L
L
L
L
α+α’
α+α’
L1 +L2
(a)
(b)
(c)
(d)
(e)
Effect of Ωl and Ωs on the phase diagram
Ωl =--20
Ωs =30
Ωl =-10
Ωs =30
Ωl =0
Ωs =30
Ωl =10
Ωs =30
Ωl =20
Ωs =30

## Slide 37
Regular solution in both liquid and solid
(p)
(l)
(f)
the solid phase becomes increasingly less stable than the liquid phase, which deepens the depression of the liquidus and solidus curves and eventually forms a eutectic.
Ωs =-15
Ωl =-20
Ωs =0
Ωl =-20
Ωs =+15
Ωl =-20
L
Ωs,l，[kJ]