## Slide 1
Weishu Liu
Department of Materials Science and Engineering
Southern University of Science and Technology (SUSTech)
Email: liuws@sustech.edu.cn
Office: North Tower,Rm310
Lecture 17: Phase diagram-III
MSE 311: Thermodynamics of Materials

## Slide 2
46. Formation of a new compound
Chapter 13.6
Binary system contanning compounds
Ref. Introduction to the thermodynamics of Materials, 6th edition, D. R. Gaskell, and D. E. Laughlin

## Slide 3
Binary phase diagram contains a compound
Mg-Si phase diagram

## Slide 4
ΩAB =0
-2RT
2RT
Equation of binodal curve
Equation of sipnodal curve
(A,B )
Solid solution
A/B
Phase separate
AB new phase

## Slide 6
The calculation of the Mg-Si phase diagram
The phase diagram for the system Mg– Si is shown in Fig. 13.14. Determine the extent to which the phase diagram can be calculated, assuming that the liquid solutions exhibit regular solution behavior
Magnesium melts at 921 K:
Silicon melts at 1688K;
Mg2Si melts at 1358K;
The standard Gibbs free energy change for the reaction
Regular solution approximation

## Slide 7
(ii)
T=1358K
Mg
Si
Mg2Si
The equilibrium equation
Since liquids on the Mg2 Si liquidus line are saturated with Mg2 Si, aMg2Si ( s) =1
Determined the interaction parameter Ω in the liquid solution
The calculation of the Mg-Si phase diagram

## Slide 8
The calculation of the Mg-Si phase diagram
T=1358K
T=1358K: Liquid Mg + Solid Si
standard state
Mg
Si
Mg2Si
Gibbs energy of
mixing liquid Mg-Si
At=1358K, Liquid Mg + Solid Si as standard
The formation energy of Mg2/3 Si1/3 from Liquid Mg + Solid Si
Line de:
Line cd:
Line ce:

## Slide 9
The calculation of the Mg-Si phase diagram
Line ce:
The formation energy of Mg2/3 Si1/3 liquid solution
from Liquid Mg + liquid Si, at T=1358K
* The interaction parameter Ω=-53,040 [J]
T=1358K
Mg
Si
Mg2Si

## Slide 10
(ii)
Since liquids on the Mg2 Si liquidus line are saturated with Mg2 Si, aMg2Si ( s) =1
Regular solution approximation
Ω=-53,040
T=1358K
Mg
Si
Mg2Si
Mg2 Si liquid line
The calculation of the Mg-Si phase diagram

## Slide 11
Si liquid line
Since liquids on the Si liquidus line are saturated with Si, a Si ( s) =1
Mg liquid line
Since liquids on the Mg liquidus line are saturated with Mg, a Mg( s) =1
The calculation of the Mg-Si phase diagram
T=1358K
Mg
Mg2Si

## Slide 12
47. Phase diagram of multi elements
微观组织热力学，西泽泰二，化学工业出版社
相图理论及其应用， 王崇琳，高等教育出版社

## Slide 13
Phase diagram of multi elements
Single element two phase
Phase I
Phase II
Phase α
Phase β
two elements two phase
Three elements two phase
Phase α
Phase β

## Slide 14
Three elements Three phase
Phase α
Phase β
Phase γ
Phase diagram of multi elements
For the system with n elements

## Slide 15
Phase diagram of multi elements
Ternary element molar free energy:
General formula:

## Slide 16
Composition triangle
Concentration triangle or Gibbs triangle
zA + zB + zC =1
zA =20%
zB =30%
zC =50%

## Slide 17
Gibbs phase law in ternary system
平衡相区 | 相数P | p-T-x |  | T=const. or P=const. | 
 |  | f | 平衡特性 | f | 平衡特性
单相区 | 1 | 4 | 四变平衡 | 3 | 三变平衡
双相区 | 2 | 3 | 三变平衡 | 2 | 二变平衡
三相区 | 3 | 2 | 二变平衡 | 1 | 一变平衡
四相区 | 4 | 1 | 一变平衡 | 0 | 零变平衡
五相区 | 5 | 0 | 零变平衡 | - | -
f=C-P+2

## Slide 18
Tie line and Lever rule

## Slide 19
Tie triangle in ternary system
α, β, γ: new phases
Tie (结线)：

## Slide 20
Ternary complete liquid and solid solutions
(三元均晶相图)
1. Binary boundary systems

## Slide 21
Isothermal section

## Slide 22
Vertical section
T/ oC
80A
20C
80B
20C
注: 不能随便在垂直界面上标注表示结线的水平线

## Slide 23
Space model

## Slide 24
Ag-Au-Pd system

## Slide 25
Ternary system with Eutectic point
Melting grooves ( 熔化沟)
Univariant line
Univariant valleys

## Slide 26
Ternary system with Eutectic point

## Slide 27
CaO-MgO-MnO

## Slide 28
Ternary system with two Eutectic points

## Slide 30
Ternary system with two Eutectic points

## Slide 32
Ternary system with three Eutectic points
Binary boundary eutectic point: e1, e2, e3
Ternary four phase eutectic point: E
Eutectic line ( melting grooves) : e1E, e2E, e3E
Filed of primary crystallization

## Slide 33
Ternary system with three Eutectic points
Reaction scheme is introduced by E. Scheil 1936.
利用零变平衡和相应的单变平衡来表示相平衡关系

## Slide 34
L
L+β
L+α
α+ β
α
α
L
α
β
γ
4-phase region: L+α+β+γ

## Slide 35
48. General Rule of Phase diagram
微观组织热力学，西泽泰二，化学工业出版社
相图理论及其应用， 王崇琳，高等教育出版社

## Slide 36
Lev D. Landau，
1908-1968
Landau phase boundary relationship
R1 ： dimension of the phase boundary (相邻相界维数)，
eg. R1 =2 for area ； R1 =1 for line; ； R1 =0 for point
R: dimension of phase diagram or section
D- ： phase decrease across the boundary
D+ ： phase increase crease across the boundary
Region I Region II, increase a phase：
D+=1, R=2, R1=1
Region IV Region II, decrease a phase
D-=1, R=2, R1=1
Region I Region IV, increase two phase ：
D+=2, R=2, R1=0
R=2

## Slide 37
General rule of ternary phase diagram
single phase (f=3):
It connected with 4-phase region at a point，
eg. L and L+α+β+γ connected at L ; α and L+α+β+γ connected at a
It connected with 3-phase region at a line，
eg. L and L+ α+β connected at e1L melting grooves
It connected with 2-phase region at a area
eg. L and L+ α connected at a area
It connected with 1-phase region at pole

## Slide 38
General rule of ternary phase diagram
two phase region (f=2):
It connected with 4-phase region at line，
eg. α+β and L+α+β+γ connected at a-b line
It connected with 3-phase region at area，
It connected with 2-phase region at a curve
e.g. α+β and α+γ

## Slide 39
Landau phase boundary relationship

## Slide 40
Extension line rule
1915年 Schreinmakers 从热力学上证明延长线法则
1940年1944年， Lipon和Wilson 分别从相平衡角度证明该法则
The extension line of boundary of the single phase
can enters 3-phase region，or two other two 2phase region
can’t enters another 1-phase region or one 3-phase region + one 2-phase region
The included angle (夹角) of extension lines of boundary of the single phase
should be less than 180 o